Carcoon Australasia

Technical Specs:

Indoor unit

• Specially manufactured Clear PVC to BS1763 Type B specification.

• Antistatic additive: UV stabilized, cold track tested to –20 degrees Celsius.

• Base material: Polyplax double coated reinforced 610

• Main zipper: size 10, 8mm spiral steel closer (inflatable units) size 5, 5mm spiral steel closer (Drive-in units)

• Air treatment units: two units per Carcoon

• Primary filter: high performance Polypure FRS60, surface area 148 sq. in.

• Secondary filter: FRS20 surface area 44 sq in.

• Constant return filter: Carbotec activated carbon FB1V surface area 30 sq. in.

• Fan/ventilator: 12 volt brushless 200 mA

• MTBF 50,000 hours constant at 33cfm

• Fan mounting: Anti-vibration 9 mm foam plan

• Return air speed through carbon filter: 1.5 mph constant (storage mode)

- Mild steel powder coated frame to Drive-in Units

Technical Specs:

Outdoor unit, outer material

Vitapruf 529

| #### Description | Woven nylon coated with hydrolysis resistant modified silicone elastomer pigmented silver. |
| --- | --- |
| Base fabric | 65gsm Nylon, 110 dtex yarn warp and weft. |
| Coating | 40gsm Hydrolysis resistant modified silicone elastomer. |

| Property | Test Method | Requirement | Typical Result |
| --- | --- | --- | --- |
| Width | BS 3424 : Part 1 Method 1* | 135 (min) | 135 |
| Total mass | BS 3424 : Part 3 Method 5A* | 105 - 115gsm | 105 |
| Tensile strength | BS 3424 : Part 4 Method 6A* | Warp : 620N (min) Weft : 530N (min) | 670 600 |
| Tear strength | BS 3424 : Part 5 Method 7B | Warp : 100N (min) Weft : 100N (min) | 150 150 |
| Cold crack | BS 3424 : Part 8 Method 10A | -40OC (max) | -50 |
| Resistance to water penetration | BS 3424 : Part 26 Method 29C* | 80cm (min) | 100 |
| Blocking | BS 3424 : Part 11 Method 13* | Surfaces to separate | Pass |
| Colour fastness to light | BS 1006 BO2 | 5 - 6 | 5 - 6 |

© Carcoon Australasia 
Freecall: 1800 888 009, Ph 617 5537 7766: +617 5537 7799

Showroom 25/38 Kendor Street, Arundel Qld 4215.

Email: info@carcoon.com.au,

www.carcoon.com.au